## Slide 1
14-NM TECHNOLOGY
& FinFET in MICROWIND
Etienne.sicard@insa-toulouse.fr

## Slide 2
Technology node | Year of introduction | Key Innovations
90nm | 2003 | SOI substrate
65nm | 2004 | Strain silicon
45nm | 2008 | 2nd generation strain, 10 metal layers
32/28nm | 2010 | High-K metal gate
20nm | 2013 | Replacement metal gate, Double patterning, 12 metal layers
14nm | 2015 | FinFET
MICROWIND APPLICATION NOTES
www.microwind.org > Application Notes

## Slide 3
Microwind’s 14-nm rule file has been tuned to the 14-nm technology information based on available publications
The FinFET has been introduced in Microwind
Layout, size and performances inspired from 14-nm FinFET proposed by IMEC, Belgium, Princeton University, USA,
14-NM APPLICATION NOTE
Standard cell level parasitics assessment in 20nm BPL and 14nm BFF
P. Schuddinck, IEDM 2012
3-D-TCAD-Based Parasitic Capacitance Extraction
for Emerging Multigate Devices and Circuits
Ajay N. Bhoj, IEEE VLSI, Vol 21, N°11, 2013

## Slide 4
Technology
Complexity
Packaging
2004
130nm
100M
Core+ DSP
1 Mb Mem
Embedded blocks
2007
90nm
250M
Core DSPs
10 Mb Mem
2010
45nm
500M
Dual core
Dual DSP
RF
Graphic Process.
100 Mb Mem
Sensors
2013
28nm
2G
Quad Core
Quad DSP
3D Image Proc
Crypto processor
Reconf FPGA,
Multi RF
1 Gb Memories
Multi-sensors
14nm
2016
7G
5nm
150 G
2020
?
Mobile generation
3G
3G+
4G
4G+
5G
This application note

## Slide 5
MOS
Current drive (mA/µm)
2.0
1.0
0.0
130 nm
1.5
0.5
45 nm
65 nm
20 nm
32 nm
14 nm
Technology node
Intrinsic performances
Strain
Gate material
90 nm
Strain to increase mobility
High K Metal Gate to increase field effect
FinFET for increasing drive current and reducing leakage
Ioff: 100nA/µm
10 nm
High performance
Low power
10nA
1 nA
This application note
General Purpose
MOS CURRENT DRIVE

## Slide 6
Microwind works in lambda units (λ)
Not optimum but independant of technology
Design rules have remained nearly the same for 20 years
λ =8nm in 14-nm technology (nearly half)
Channel length is 2 λ
Minimum gate pitch is 8 λ (2+6)
Minimum metal pitch is 6 λ (3+3)
14-NM TECHNOLOGY IN MICROWIND
Gate pitch
Metal
pitch
Channel length

## Slide 7
FROM MOSFET TO FINFET
The FinFET device has a different layout style than the MOS device
Instead of a continuous channel, the FinFET uses fins
FinFET provides the same Ion current at a smaller size
FinFET provides lower leakage current Ioff at the same Ion
fins

## Slide 8
INTRODUCING THE FINFET
MOS Parameter | Typical value
Width (W) | 6 - 12 λ
Length (L) | 2 λ
FinFET Parameter | Typical value
Number of fins (NF) | 2 - 5
Fin pitch (PF) | 6 λ
Fin thickness (TF) | 1 λ
Fin length or gate length (LG) | 2 λ
New screen in Microwind

## Slide 9
3D OF FINFET USING MICROWIND
Gate
Drain
Source
Fin 1
Fin 2
Fin 3
Fin 4
N-FinFET
P-FinFET
Microwind enables a 3D view of the FinFET
Fin height (HF)
Fin thickness
(TF)
Fin length
(LG)

## Slide 10
FIN BENEFITS
Patton, Evolution and Expansion of SOI in VLSI Technologies: Planar to 3D, IEEE International SOI Conference 2012
Gate
FIN from Drain to Source
The total equivalent channel width is higher in FinFET than in MOSFET
Weq = 2*HF+TF
Benefit around 30% in current drive
Fin height (HF)
Fin thickness
(TF)
Total equivalent channel width Weq
Ion
Ioff
MOS
Fin

## Slide 11
GENERATING A FINFET
Fin Length, equal to gate length, (LG) is 2 lambda (16 nm) by default
Fin thickness (TF) is set to 1 lambda (8 nm)
Fin pitch (PF) is set to 6 lambda (48nm)
FinFET comme with dummy gates for manufacturability

## Slide 12
HD: High density drawing style : 2 fins
HP : High performance drawing style : 4 fins
GENERATING A FINFET
1 fin exists in very high density cells such as SRAM
FinFET with more than 4 fins drive string currents

## Slide 13
Fins should be aligned and horizontal, regular pitch 6  (1+5)
Non-aligned fins may lead to gate distortion and current performance spread
FINFET MANUFACTURABILITY
Ion
Ioff
Ion
Ioff

## Slide 14
Gates should be aligned and vertical, regular pitch with 8  minimum (2+6)
FINFET MANUFACTURABILITY

## Slide 15
BSIM4 is a good model for MOS devices
BSIM-CMG is targetted to FinFET, but corresponds to a completly new model
The HFIN and TFIN parameters have been added to BSIM4 in Microwind to handle the FinFET
HFIN: Fin Height
TFIN: Fin thickness
FINFET MODEL
Fin height (HF) 30nm
Fin thickness
(TF) 10nm
With 2 fins, Weff=140nm

## Slide 16
5.0
3.3
2.5
1.8
0.35µ
0.18µ
90n
65n
Technology node
1.0
Supply (V)
1.2
45n
I/O supply
Core supply
32n
20n
14n
130n
0.8 V inside, 1.2V outside
10n
7n
14-nm technology
SUPPLY VOLTAGE SCALE DOWN
VDD is lowered to 800mV in 14-nm technology

## Slide 17
Chart: pFET Mobility (cm2/Vs)
| Relaxed Si | Relaxed Ge | Strained Si | Ge+Sn
Mobility (cm2/Vs) | 200 | 300 | 400 | 700
STRAIN
Strain enables outstanding p-FinFET mobility performances, approaching the n-FinFET mobility

## Slide 18
Metal stack
INTERCONNECTS
Main target | Pitch |  | nm | Used for
M7, M8 | 4 | 24 | 192 | Supply
M5, M6 | 3 | 18 | 144 | Long routing
M3, M4 | 2 | 12 | 96 | Medium routing
M1, M2 | 1.4 | 8 | 64 | Short routing
Gate, Local interc. | 1 | 6 | 48 | Intra-cell routing

## Slide 19
Middle of Line (MOL) Local Interconnects
New material « Local Interconnect (LI) » used for very short interconnects
Less capacitance than m1 only
More space for metal 1
10% improved cell density
LOCAL INTERCONNECT
Local interconnect Layer
Contact
Gate
M. Rashed, ‘Innovations in special constructs for standard cell libraries in sub 28nm technologies," Electron Devices Meeting (IEDM), 2013

## Slide 20
REASONS OF COST EXPLOSION
Performance improvements
  Strain
  eSiGe,
  High-K dielectric
  Metal gate
  Low-K inter dielectrics,
  FinFET
New options
  Local interconnects
New constraints
  double patterning, FinFET
TECHNOLOGY INNOVATION & COST
Chart: Relative cost of technology
| 65nm | 45nm | 28nm | 20nm | 14nm | 10nm
Cost of technology | 1 | 1.4 | 1.9 | 3 | 4.2 | 6.3

## Slide 21
Main target | Type of innovation | First order effect
Device performance | Strain | Improved n mobility
 | Embedded SiGe (e-SiGe) | Improved p mobility
 | High K gate dielectric | Increased field effect
 | Metal gate | Decreased leakage
 | FinFET | Higher current density
Interconnect performance | Low K inter dielectrics | Reduced crosstalk and delay
 | Local interconnect | Higher density
Manufacturability | Double patterning | Improved yield
TECHNOLOGY INNOVATION & COST

## Slide 22
Microwind DRC only checks 100 basic design rules
In 14-nm technology, more than 2500 design rules have been listed
DESIGN RULES
130nm
500
design rules
65nm
1000 design rules
14nm
2500
design rules

## Slide 23
Thank you for your attention
Etienne.sicard@insa-toulouse.fr